1058-8, SINGIL-DONG,                                               TEL: 82-31-491-9250

ANSAN-CITY, KYUNGKI-DO,                                         FAX: 82-31-493-6126

KOREA.

TAIYO INK MFG.CO.,(KOREA) LTD.

THERMALLY CURABLE MARKING INK

2-COMPONENTS MIX SYSTEM

S-200W / HD-3

S-200W / HD-3

1. Characteristic

S-200W is thermally curable marking ink which have excellent properties:

Superior adhesion and color retention.

2. General specification

| Main Agent | S-200W |
| --- | --- |
| Hardener | HD-3 |
| Color | White |
| Mixing Ratio | Main Agent : 100, Hardener : 8 (Weight Ratio) |
| Viscosity (After mixing) | 230PS± 15% 25℃ 65RH 180PS± 15% 25℃ 65RH |
| T.I. Value | 2.0 ± 0.2 |
| Curing Conditions | 140℃ / 20 min (Hot Air Convection Oven) |
| Pot Life * | 5 hours after mixing |
| Shelf Life | 6 month after manufacturing (below 20℃ in dark room) |

* : Stored in cool and dark place at less than 25℃.

3. Process

-  Pre-treatment  : Acid Treatment → Water Rinse

(If the ink printed on Cu foil)

-  Screen Printing : 225 Mesh-counts/Inch.

-  Post Cure      : 140℃/20 min. (Hot Air Convection Oven)

4. Attention Process

-  As to the operation environment, it is desirable to deal with ink in the clean

room and 25℃is recommendable temperature conditions and 50 ~60% rh is

recommendable humidity conditions for printing.

-  The adequate thickness is 15 - 20㎛ (on the cupper after curing).

Thin coating possibly reduces its solder heat resistance and acid resistance.

-  Please set the cure conditions after confirmation test because they are influe-

nced according to the type of the drying machine, the quantity of the boards

to be dried and so on.

Poor curing or over curing may cause the degradation of properties.

-  As to cleaning the screen, ether or ester solvent is used for cleaning.

-  It is desirable to use ink without dilution.   Even if you feel difficulty of pri-

nting by high viscosity, please dilute ink as little as possible ( Max 2wt% )

because over dilution may degrade properties.

-  Please stir up enough after mixing of Hardener.

5. Properties

| Item | Test Method | Test Result |
| --- | --- | --- |
| Adhesion | JIS D0202 Standard Cross-cut Tape Stripping Test | 100 / 100 |
| Pencil Hardness | JIS K5400 Standard | 5H |
| Solder Heat Resistance | Solder Float Test; Rosin Flux 260℃/10 sec. 2 cycles | O.K |
| Solvent Resistance | 1,1,1-Trichloroethane, 20℃/60 min. Scotch Tape Stripping | O.K |
| Acid Resistance | 10 vol% HCl, 20℃/60 min. Scotch Tape Stripping | O.K |
| Alkaline Resistance | 10 wt% NaOH, 20℃/60 min. Scotch Tape Stripping | O.K |
| Insulation Resistance | IPC B pattern 500V for 1min. at 25℃/60 min. Moistured Condition 25-65℃ 90%RH Impressed vol DC 100V 7days | Initial; 5.0×1012 Ω After; 5.0×1010 Ω |
| Dielectric Constant | JIS K6481 1Mhz Moisture Condition; 25-65℃ 90%RH 7days | Initial; 7.0 After ; 7.5 |
| Dielectric Dissipation Factor | JIS K6481 1Mhz Moisture Condition; 25-65℃ 90%RH 7days | Initial;0.02 After ;0.04 |

Note : The above-mentioned test data is just for reference, not to guarantee

the result.